Foam insulation value: can be defined as a U-Value or TOG value which is a measurement on how well a material resists heat flow. The higher the TOR rating the better the insulation.

Mattress foam density is a key indicator of mattress quality. A minimum foam density for a bed mattress should be 22 kg/m³ (1.37 lb./ft³).

The firmness is defined by the indentation load deflection. This factor is the amount of force required to indent a sample of foam to 25% of its original height. It may vary from 5 to 100 kg

| Foam Specifications |  |
| --- | --- |
| Material: | PPE (Polyphenylene Ether) |
| Type: | Closed cell |
| Density: | Foam density is a key indicator of mattress quality. A High density > 27 kg/ m3 |
| Thickness: | Min.10-12mm |

Other requirementa

Covering: for covered mattresses, coverings should be easily removable to allow them to be washed.

Fire: mattresses should not produce toxic fumes when burnt and should not be easily flammable.

Waterproofing: all mattresses and mats should be kept dry by ensuring that they are separated from the ground by a waterproof membrane. Additional plastic sheeting, timber or cement may be required to separate the bedding from the ground