General information The shelter tool kit has been designed by IFRC for distribution after a disaster. It is designed for one kit per family. Summary Specifications SPECIFICATIONS; Quantity per Kit; Units; Indicative Picture. TARPAULINS, woven plastic, Width 4 m Length Sheet of 6 m. Weight 170g/m2 +/- 5%, plus 10% for the reinforcement bands under ISO 3801.; 2; pc. ROPE, nylon, diameter: 12 mm, 30m, in roll, Preferred colour: Black / Dark Green. Three strings possibility to untie; 1; roll. HAND SAW, total length 750mm, for wood, Good Quality, tempered, hardened and set teeth. Unbreakable handle. Blade covered by protective cardboard; 1; pc. CLAW HAMMER, Weight: 0.750 kg/pc. Replaceable Wooden handle. Forged head, not cast. Good Quality; 1; pc. SHOVEL, head only is hot forged carbon steel, hardened and tempered. HRC 35min to 48 max. Supply with handle. With pointed head. Total length 100 to 110 cms; 1; pc. HOE, head only is 230 x 175 mm, 1.360g in forged steel, Supply with varnished hard wood handle length approx. 110-120cm, supply blade covered by cardboard; 1; pc. SHEARS, straight, for metal sheet, semi-hard 1mm max., 255mm; 1; pc. Cutting knife, wooden handle, supply blade covered with protective cardboard; 1; pc. ROOFING NAILS, Capped, with attached rubber washer 75mmx3mm (3’’), twisted and galvanised preferred, to be supplied in sealed bag.; 0.5; kg. NAILS, 0,5 kg Steel, 3 inches long (75 x 3mm), to be supplied in sealed bag.; 0.5; kg. NAILS, 0,5 kg Steel, 40mm long (40 x 2mm), to be supplied in sealed bag.; 0.5; kg. TIE WIRE, Diameter 1,5mm. 25m long in roll; 1; roll. Packing and Shipping Specification. Particulars; Weight per Carton KG; Size Carton (mtrs); Volume per carton; Payload per 40'DC Container. 2 Kits Packed Per Carton / 1 Kit - approximate weight - 11.1 KG; 22.2; 1.2 x 0.3 x 0.2; 0.072; 1750 Kits. Detailed Specifications for Tools ROPE, polypropylene, black, 12mm diam., twisted. Diameter:; 12mm +/- 0.5mm. Length:; 30m. Weight:; 1.9kg. Number of strand:; 3 minimum. Type:; twisted. Material:; polypropylene, no recycled fibres, UV stabilized. Colour:; black. Tensile strength:; 300kg. HANDSAW, for timber. Type & dimensions:; carpenter handsaw, 400-450mm blade, lacquered, overall length 550mm +/-50mm. Blade thickness:; 1mm +/- 0.05mm, protected against oxidation. Blade protection:; Protective cardboard, teeth protection with hard, plastic cover.. Seal type:; laminated carbon steel, hardened and tempered. Number of teeth:; 7-teeth per inch. Quality of make:; Soft edges but no dents, cracks or broken teeth. Hardness Rockwell C:; 45 to 50 HRC for the whole blade, 48 to 52 HRC at teeth level. Carbon content:; 0.47% to 0.55%. Manganese content:; 0.5% to 0.8%. Handle:; Wooden dismountable handle, minimum 3 fixations, polished varnish hardwood, large 85x35mm opening for hand comfort when wearing gloves. Optional 45/90° square. Moisture minimum 10%, maximum 15%.. Strength testing:; With the blade inserted into a 10mm-wide slot to a depth equal to 1/3 the blade's length, but not exceeding 150 mm, a deflection of 90° is applied 25 times in each direction without breakage or permanent set to the blade.. NAIL, FOR ROOF SHEETS, galvanized with watertight rubber washer, umbrella type. Type:; Iron nails, made of polished low-carbon steel, cold processed, not heat treated except for galvanization.. Shape:; Spiral rolled or twisted shank, sealed umbrella-type spring-head.. Corrosion treatment:; hot-dip galvanized at 300g/m2 +/-10%. Tensile strength:; minimum 650N/mm2. Accessories:; attached rubber washer with each nail. Dimensions (+/-5%):; shank: 75x3.6mm, head diameter: 20mm minimum. Rubber washer:; diameter 26mm x thickness 2mm. Packing:; packed in a strong, thick PE 130g/m² plastic bag, which can be zipped or locked. Quantity:; net weight: 0.5kg. SHOVEL, round point with Y handle. Material:; Pressed carbon-steel, hardened and tempered. Corrosion protection:; black paint. Quality of make:; no excess metal in the eye, no dents, no cracks, soft edges. Hardness Rockwell C:; 35 minimum to 48 maximum HRC. Carbon content:; 0.4% to 0.6%. Manganese content:; 0.5% to 1%. Silicone:; 0.37% maximum. Phosphorus & Sulphur:; 0.06% maximum. Dimensions, full piece:; 295 x 225mm +/-15mm. Hole diameter:; front side 36mm, back side 40mm, +/-5%. Weight:; 1kg +/- 50g, without handle. Strength testing: - Using a fitted, standard hardwood handle, clamp the blade of the shovel near the handle in a horizontal position. Gradually apply a load of 45kg and maintain it for 2 minutes. This should not result in any damage to the blade or a loosening of the handle, and no permanent set in excess of 25mm. - With one centimetre of the end of the blade secured in a clamp, move the handle back and forth 30 degrees. There should be no permanent set greater than 25mm. With the shovel held in a digging position, a 37mm in diameter piece of wood is hit hard against it. The blade should not buckle or break.. Handle: No chips, rough surfaces, cracks, holes or knots. Smooth, polished varnish surface. Dry, strong and flexible wood. Moisture minimum 10%, maximum 15%. Handle adapted to head so that it can be blocked and secured with a nail. Total length 1070mm +/- 50mm (head included). The other end of the handle is made in a Y-shape with same quality of wood. The branches of the Y handle must be made of good-quality iron, securely fitted to the handle.. HOE, with long handle, large type. Material:; hot forged carbon steel, hardened and tempered, at a maximum the hardened zone should reach halfway up the back of the blade. Corrosion protection:; black paint. Quality of make:; no excess metal in the eye, no dent on the cutting edge, reinforced head with a rib from the eye to the middle of the blade length. Hardness Rockwell C:; 35 minimum to 48 maximum HRC in hardened zone of the blade. Carbon content:; 0.5% to 0.8%. Manganese content:; 0.6% to 1.2%. Silicone:; 0.37% maximum. Phosphorus & Sulphur:; 0.06% maximum. Dimensions, full piece:; 180 x 310 mm +/-10mm including the eye. Hole diameter:; high raised neck, front side 43 mm, back side 48 mm+/-2mm. Weight:; 1.250kg +/- 150g, without handle, depending on the type of hoe. Strength testing: - Using a fitted, standard hardwood handle, clamp the blade of the hoe near the handle in a horizontal position. Gradually apply a load of 45kg and maintain it for 2 minutes. This should not result in any damage to the blade or a loosening of the handle, and no permanent set in excess of 25mm. - With one centimetre of the end of the blade secured in a clamp, move the handle back and forth 30 degrees. There should be no permanent set greater than 25mm. With the hoe held in a digging position, a 37mm in diameter piece of wood is hit hard against it. The blade should not buckle or break. Handle: No chips, rough surfaces, cracks, holes or knots. Smooth, polished varnish surface. Dry, strong, and flexible wood. Moisture minimum 10%, maximum 15%. Handle adapted to head so that it protrudes from and blocks on the other side of the head. Total length 1100mm to 1150mm.. Cutting Blade. Type:; curved blade, lacquered against oxidation. Blade thickness:; 2.5mm thick. Handle:; wooden handle. Material:; hot forged carbon steel, hardened and tempered, hardened throughout the entire blade, but remains normal past the first rivet hole.. Quality of make:; no dent on the cutting edge. Hardness Rockwell C:; 45 minimum to 50 maximum HRC near cutting edge, test 3 positions along the cutting edge. Carbon content:; 0.48% to 0.65%. Manganese content:; 0.6% to 1%. Silicone:; 0.37% maximum. Phosphorus & Sulphur:; 0.03% maximum. Handle: No chips, rough surfaces, cracks, holes or knots. Smooth, polished varnish surface. Dry, strong, hardwood. Moisture minimum 10%, maximum 15%. Strength testing: Insert the blade in a 10mm-wide slot up to a depth equal to 1/3 its blade length, but not exceeding 150mm; apply a deflection of 45° in each direction without breakage or permanent set to the blade.. SHEARS, straight, for metal sheet, semi-hard 0.8mm max., 260mm. Type:; tin snips for intensive use and easy maintenance. Make:; each blade and handle forged as one piece, symmetrical blades. Capacity:; up to 0.8mm semi-hard iron sheet. Material:; hot forged carbon steel, hardened and tempered, special treatment applied to the blade edge. Rustproof:; protected against corrosion with special paint. Dimensions:; overall length: 250 to 260mm. Maintenance:; dismountable in 2 parts only, with bolt and self locking nut. NAIL, iron, for wood, large. Type:; iron nails, made of polished low-carbon steel, cold processed, not heat treated except for galvanization. Rustproof:; hot dip galvanized at 300g/m2 +/-10%. Tensile strength:; minimum 650N/mm2. Shape:; flat, smooth, circular head; plain, round shank and diamond point. Dimensions (+/-5%):; ll length x diameter: 75x3.6mm, head diameter: 7.7mm. Packing:; packed in strong, thick PE 130g/m² plastic bag, which can be zipped or locked. Quantity:; net weight: 0.5kg per type. NAIL, iron, for wood, small. Type:; iron nails, made of polished low carbon steel, cold processed, not heat treated except for galvanisation.. Rustproof:; hot dip galvanised at 300g/m2 +/-10%. Tensile strength:; minimum 650N/mm2. Shape:; ll flat smooth circular head, plain round shank and diamond point.. Dimensions (+/-5%):; ll length x diameter: 40x2.2mm, head diameter: 5mm to 5.5mm. Packing:; packed in strong thick PE 130g/m² plastic bag, which can be zipped or locked. Quantity:; net weight: 0.5kg per type. TIE WIRE, galvanised, diam. 1.5 mm, 25m, roll. Material; ll low carbon steel, hot dip galvanised with minimum 40g/m2, binding /tie wire.. Quantity; roll of 25m.. Dimension; diameter 1.5mm +/-5%. Tensile strength; minimum 340 N/mm² to Maximum 500N/mm. CLAW HAMMER. Type:; Carpenter hammer, head and handle, hammer head with flat and claw side, as per ISO15601, except for the pull-apart test force.. Material:; high-carbon steel head, treated to achieve a martensitic structure, with dressed striking faces. Quality of make:; smooth surface and edges with no dents or cracks; no excess metal in the eye. Weight of the hammer:; Total weight 750g +/- 50g (equivalent to 700g minimum, 800g maximum). Hardness Rockwell C:; 50 minimum to 58 maximum HRC on striking faces. Hardness Rockwell C:; 35 maximum HRC closed to the eye. Handle: No chips, rough surfaces, cracks, holes or knots. Smooth, polished varnish surface. Dry, strong, and flexible wood. Handle adapted to head so that it protrudes and can be blocked on other side with a metal wedge on the other side of the head. Moisture minimum 10%, maximum 15%.. Pull-apart test: ISO15601. After two series of 25 vigorous blows with varying delivery angle, secure head in a clamp, apply a minimum traction of 50kg trying to pull the handle out. This should not damage the hammer head or the handle, and the handle should remain firmly attached to the head.. Bending test: ISO15601. For the claw hammer only, apply a load perpendicularly to the axis of the handle and close to the end, so as to obtain a 125Nm torque, irrespective of the size of the hammer. Start the load at zero and increase gradually, without jerking. Hold the test load for at least 10s. This should not create any damage to the hammer head or handle.. POLYETHYLENE BAG (1 bag per kit). Material:; Standard ICRC/IFRC tarpaulin, white, without the bands. Type:; Square rectangular base duffle bag with 6 aluminium or galvanised steel eyelets and a 10mm PP rope for closing that can also act as a shoulder handle.. Dimensions:; Total length 1250mm Final packed maximum dimension 1200x300x150mm +/-10mm. The closing rope of the bag can be detached from the bottom of the bag and packed inside the mouth of the bag. The bag is securely sealed with a plastic strap with manual opening.. Includes a copy of the content list for the complete shelter kit printed on the outside of the bag; and a copy of the user's instruction, printed on durable textile or laminated paper, placed inside the bag. Original user's instruction document available in here below attachment “specifications.pdf”. Customer's marking and logo printed on the outer bag in durable printing. Tarpaulins are not packed in this bag.. CARDBOARD FOLD (1 per kit). Material:; Double-walled corrugated cardboard.. Type:; One or several pieces of cardboard in which the complete kit is securely packed before being placed in the bag. The cardboard folds on the 2 long sides and one short side.. Dimensions:; To fit in the outer bag. Sealing:; Strapped with 2 heat-sealed 10mm minimum plastic straps.. Quality:; Loaded cartons should withstand 1m-high stacking on pallets, and several handlings (hand and forklift) without damage. Palletising:; The pallets (wood or metal) are made or reinforced in such a way that allows 2 levels stacking (stacking up to 2m high), without any damage for the kits and the kit packaging.. Remark: Tarpaulins are packed separately..

Content list - Export content list (excel file). Code; Description; Qty. APACBAGSPE180; 1. EHDWNAILRS01; "NAILS, ROOFING, 75mm (3""), hot galva. + rubber washer, 0.5kg"; 1. EHDWNAILW040; "NAILS, hot galvanised iron, for wood, 40mm, (1.1/2"") 0.5 kg"; 1. EHDWNAILW080; "NAILS, hot galvanised iron, for wood, 8cm (3""1/6), 1kg"; 1. EHDWWIRETR15; TIE WIRE, galvanised, diam. 1.5 mm, 25m, roll; 1. ETOOCUTTSHE1; SHEARS, straight, for metal sheet, semi-hard 1mm max., 255mm; 1. ETOOHAMMCARW; HAMMER, nail claw, carpenter type, 750g, wood handle; 1. ETOOSAWSW400; SAW, for timber, 400mm blade; 1. HSHEROPE12PB; ROPE, POLYPROPYLENE, black, diam. 12mm, twisted; 30. RAGRTOOLHOE3; HOE, with long handle, large type; 1. CUTTING BLADE, approx. length 500mm, wooden handle; 1. RAGRTOOLSHO2; SHOVEL, round point with Y handle, total length approx.1m; 1..