Technical Working Group-  29th October 2013

| Tool Kit: Recovery & Rubble Removal |  |
| --- | --- |
| Tool Type | Specification |
| General |  |
| Claw Hammer | Local specification |
| Timber saw | SAW, for timber, 400mm blade/ SAW, bow type, for wood, 450mm blade |
| Nails | Common wood nails, umbrella nails, (roofing with rubber washers) 40mm/75mm |
| Wire - Tie wire | Galvanised, diam. 1.5 mm, 25m, roll |
| Rope | Polipropilene,12 mm twisted |
| Clean up and rubble removal |  |
| Empty rice bags | Local |
| Wheelbarrow | Approx. 90l dry solids, strong solid wheel |
| Hack saw - blades | Steel bar frame, wood handle, wing nut, L. 300mm/ 24” |
| Bolo – Philippine knife | Local specification |
| Barra | Twisted Steel Bar with a chisel on the end |
| Crow bar | With angled beak, 300 mm length/with angled beak, 500 mm length |
| Cold Chisel | Flat 20mm, for masonry, 300mm length/1” |
| Sledge hammer | Hardened steel, wood handle, 4800g, 900mm/hardened steel, wood handle, 1200g, 250mm |
| Shovel /Spade | Square faced shovel total length approx.1m |
| Personnel protection |  |
| Gloves | Protection, heavy duty soft leather, size 11, pair |
| Goggles | Plastic, with rubber string, eyes protection |
| Mask | Vapour and dust protection, FPP2 disposable half mask |
| Boots | Heavy duty plastic rubber, pair, size various |

Tarpaulins:

- Individual unit size 6x4m

- Weight : 180g/m² ± 30g under I SO 3801

- Material: Woven high-density polyethylene (HDPE) black fibers fabric + laminated on both sides with white low density polyethylene (LDPE) coating.

- Tensile Strength: Minimum 500N and 15% to 25% elongation in warp and weft in plain sheet under ISO 1421-1.

- Tear Strength: Minimum 100N under I SO 4674-1 2003, strip of 200x200mm, in plain sheet

- Welding: Only one welding allowed, in the middle of the sheet, lengthwise. The tarpaulin tensile strength crossways at the place of the welding under ISO 1421-1 must be: Minimum 50% of the original value of the actual product, AND not less than 400N.

- UV Resistance: The tarpaulin tensile strength under I SO 1421-1 after 1500 hours UV under ASTM G53/94 (UVB 313 nm peak) must be: Minimum 80% of the original value of the actual product, AND not less than 475N. To be tested in the plain sheet.

- Temperature resistant : From 20 to 80 degrees Celsius

- Flammability: Flash point above 200 degrees Celsius